Supporting information of

New strategy of getting accurate refractive indices dispersion curve using first-principles sun-over-states jointed with density functional perturbation theory

Yu-Ju Hsieh†, Ming-Hsien Lee*

Department of Physics, Tamkang University, New Taipei City, 25137, Taiwan

*Corresponding author e-mail address: mhslee@mail.tku.edu.tw

More materials with their convergence tests and calculation results are listed here. The plane wave cutoff energies and the k-points of the other materials are given in Table S1 and S2. The refractive indices and birefringence of various materials have been calculated using the sum-over-states (SOS) method and the density functional perturbation theory (DFPT) method, and the results are summarized in Table S3. Fixed symmetry DFPT results for other materials are shown in Table S4.

Table S1: the refractive index corresponding to different cut-off energies, k-points, different funtionals, ionic contribution, electronic contribution and fixed crystal symmetries are calculated for LiNbO3, LiGaSe2 and BPO4 materials by DFPT.

| compound | functional | Cut-off energy | k-point | no-Efield | ne-Efield | no-SOS | ne-SOS |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BPO4 | GGA | 830 | 14×14×16 | 1.611 | 1.622 | 1.662 | 1.65 |
| BPO4 | GGA | 830 | 9×9×11 | 1.611 | 1.622 | 1.662 | 1.65 |
| BPO4 | GGA | 830 | 7×7×8 | 1.611 | 1.622 | 1.662 | 1.65 |
| BPO4 (ionic) | GGA | 830 | 7×7×8 | 1.611 | 1.622 | 1.662 | 1.65 |
| BPO4 | GGA | 750 | 7×7×8 | 1.611 | 1.622 | 1.662 | 1.649 |
| BPO4 | GGA | 600 | 7×7×8 | 1.612 | 1.624 | 1.664 | 1.651 |
| BPO4 | LDA | 830 | 7×7×8 | 1.616 | 1.624 | 1.672 | 1.66 |
| LiNbO3 | GGA | 750 | 12×12×12 | 2.479 | 2.382 | 2.748 | 2.555 |
| LiNbO3 | GGA | 750 | 8×8×8 | 2.479 | 2.382 | 2.748 | 2.555 |
| LiNbO3 | GGA | 750 | 6×6×6 | 2.479 | 2.382 | 2.748 | 2.555 |
| LiNbO3 (ionic) | GGA | 750 | 6×6×6 | 2.479 | 2.382 | 2.748 | 2.555 |
| LiNbO3 | GGA | 830 | 6×6×6 | 2.479 | 2.382 | 2.748 | 2.555 |
| LiNbO3 | GGA | 600 | 6×6×6 | 2.48 | 2.385 | 2.751 | 2.559 |
| LiNbO3 | LDA | 750 | 6×6×6 | 2.462 | 2.361 | 2.722 | 2.528 |
| LiGaSe2 | GGA | 880 | 7×6×8 | 2.344 | 2.402 | 2.598 | 2.603 |
| LiGaSe2 | GGA | 880 | 5×4×5 | 2.342 | 2.403 | 2.599 | 2.603 |
| LiGaSe2 | GGA | 880 | 4×3×4 | 2.356 | 2.398 | 2.598 | 2.603 |
| LiGaSe2 (ionic) | GGA | 880 | 4×3×4 | 2.361 | 2.397 | 2.597 | 2.601 |
| LiGaSe2 | GGA | 800 | 4×3×4 | 2.356 | 2.398 | 2.597 | 2.603 |
| LiGaSe2 | GGA | 590 | 4×3×4 | 2.345 | 2.391 | 2.592 | 2.598 |
| LiGaSe2 | LDA | 880 | 4×3×4 | 2.422 | 2.46 | 2.679 | 2.682 |

Table S2: the k-point and cutoff energies of these materials

| compound | cutoff energy(eV) | k-point |
| --- | --- | --- |
| TiO2 | 830 | 5×5×8 |
| YVO4 | 830 | 5×5×5 |
| CaCO3 | 880 | 6×6×6 |
| BiB3O6 | 830 | 7×7×4 |
| α-BaB2O4 | 830 | 4×4×4 |
| β-BaB2O4 | 830 | 3×3×3 |
| KTiOPO4 | 830 | 2×4×2 |
| KBe2BO3F2 | 940 | 7×7×7 |
| AgGaS2 | 830 | 5×5×6 |
| CsLiB6O10 | 830 | 4×4×3 |
| AgGaSe2 | 880 | 5×5×6 |
| LiGaS2 | 880 | 4×3×4 |
| LiGaTe2 | 880 | 4×4×6 |
| LiB3O5 | 830 | 3×3×5 |
| BaMgF4 | 990 | 6×6×4 |
| SiO2 | 830 | 6×6×6 |
| Al2O3 | 830 | 6×6×6 |
| Ba2TiSi2O8 | 830 | 3×3×5 |
| Li2B4O7 | 830 | 4×4×4 |
| ZrSiO4 | 830 | 6×6×5 |
| CaMgSi2O4 | 990 | 4×4×5 |
| NaAlSi2O4 | 830 | 4×4×5 |
| LiAlSi2O4 | 830 | 4×4×5 |
| Al2O(SiO4) | 830 | 4×3×5 |
| BeAl2O4 | 830 | 3×5×6 |
| KAlSi3O8 | 830 | 3×2×4 |
| Al2Be3Si6O18 | 830 | 3×3×4 |

Table S3: The birefringence and refractive indices of experimental and calculated by the DFPT and SOS method.

| Compound | Space Group | no | ne | Δn-Efield | no | ne | Δn-SOS | Experimental value |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TiO2 | P42/mnm | 2.6738 | 2.9386 | 0.2648 | 2.806 | 3.0611 | 0.2551 | 0.256 |
| YVO4 | I41/amd | 1.9676 | 2.2051 | 0.2375 | 2.1803 | 2.4565 | 0.2762 | 0.2039 |
| CaCO3 | R3c | 1.6998 | 1.5161 | -0.1837 | 1.7855 | 1.5756 | -0.2099 | -0.172 |
| BiB3O6 | C2 | 1.7448 | 1.8701 | 0.1253 | 1.8305 | 1.9528 | 0.1223 | 0.1605 |
| α-BaB2O4 | R3c | 1.6866 | 1.5531 | -0.1335 | 1.7351 | 1.596 | -0.1391 | -0.117 |
| β-BaB2O4 | R3c | 1.7031 | 1.5683 | -0.1348 | 1.7358 | 1.5965 | -0.1393 | -0.113 |
| KTiOPO4 | Pna21 | 1.8081 | 1.9222 | 0.1141 | 1.8219 | 1.9247 | 0.1028 | 0.0921 |
| KBe2BO3F2 | R32 | 1.5099 | 1.4185 | -0.0914 | 1.5492 | 1.4801 | -0.0691 | -0.077 |
| AgGaS2 | I42d | 2.7304 | 2.7089 | -0.0215 | 3.0141 | 2.9515 | -0.0626 | -0.0532 |
| CsLiB6O10 | I42d | 1.5037 | 1.4494 | -0.0543 | 1.5475 | 1.4853 | -0.0622 | -0.049 |
| AgGaSe2 | I42d | 3.024 | 2.9902 | -0.0338 | 3.2427 | 3.2193 | -0.0234 | -0.048 |
| LiGaS2 | Pna21 | 2.3577 | 2.4074 | 0.0497 | 2.4013 | 2.4214 | 0.0201 | 0.042 |
| LiGaTe2 | I42d | 2.6638 | 2.7745 | 0.1107 | 2.9988 | 3.0041 | 0.0053 |  |
| LiB3O5 | Pna21 | 1.599 | 1.6457 | 0.0467 | 1.6544 | 1.7069 | 0.0525 | 0.041 |
| BaMgF4 | Cmc21 | 1.4768 | 1.5094 | 0.0326 | 1.5259 | 1.5419 | 0.016 | 0.0278 |
| SiO2 | P3121 | 1.5472 | 1.5555 | 0.0083 | 1.5837 | 1.5858 | 0.0121 | 0.009 |
| Al2O3 | R3c | 1.7859 | 1.7771 | -0.0088 | 1.8014 | 1.7901 | -0.0113 | -0.008 |
| Ba2TiSi2O8 | P4bm | 1.8249 | 1.7894 | -0.0355 | 1.8843 | 1.9432 | 0.0589 | -0.0003 |
| Li2B4O7 | I41cd | 1.6015 | 1.5442 | -0.0573 | 1.6509 | 1.6006 | -0.0503 | -0.0551 |
| ZrSiO4 | I41/amd | 2.0447 | 2.1032 | 0.0585 | 2.0913 | 2.1542 | 0.0629 | 0.0305 |
| CaMgSi2O4 | C2/c | 1.7153 | 1.7323 | 0.017 | 1.7594 | 1.7772 | 0.0178 | 0.0275 |
| NaAlSi2O4 | C2/c | 1.6851 | 1.7054 | 0.0203 | 1.7261 | 1.7412 | 0.0151 | 0.02 |
| LiAlSi2O4 | C2/c | 1.6917 | 1.7151 | 0.0234 | 1.7346 | 1.7452 | 0.0106 | 0.015 |
| Al2O(SiO4) | P1 | 1.746 | 1.7557 | -0.0097 | 1.7833 | 1.7749 | -0.0084 | -0.015 |
| BeAl2O4 | Pnma | 1.763 | 1.767 | 0.004 | 1.7854 | 1.7909 | 0.0055 | 0.009 |
| KAlSi3O8 | P1 | 1.5387 | 1.5452 | 0.0065 | 1.5807 | 1.5831 | 0.0024 | -0.008 |
| Al2Be3Si6O18 | P6/mcc | 1.5913 | 1.5875 | -0.0038 | 1.6122 | 1.6064 | -0.0058 | -0.006 |

Table S4: The birefringence and refractive indices of fix symmetry by DFPT. The unlabeled ones are SOS-DFPT consistent results, the other three labels are: symmetry-fixed DFPT fall back to SOS ▲, symmetry-fixed DFPT not fall back to SOS □, symmetry-fixed DFPT results in better agreement with experiment ○.

|  | Compound | Space Group | ne | no | Δn-Fix symm | Experimental value |
| --- | --- | --- | --- | --- | --- | --- |
|  | TiO2 | P42/mnm | 2.9606 | 2.7839 | 0.1767 | 0.256 |
|  | YVO4 | I41/amd | 2.2651 | 2.0733 | 0.1918 | 0.2039 |
| ▲ | CaCO3 | R3c | 1.5352 | 1.7616 | -0.2264 | -0.172 |
|  | BiB3O6 | C2 | 1.976 | 2.169 | -0.193 | 0.1605 |
|  | α-BaB2O4 | R3c | 1.6464 | 1.4685 | 0.1779 | -0.117 |
|  | β-BaB2O4 | R3c | 1.5824 | 1.7897 | -0.2073 | -0.113 |
|  | KTiOPO4 | Pna21 | 1.8992 | 1.9557 | -0.0565 | 0.0921 |
| ▲ | KBe2BO3F2 | R32 | 1.4855 | 1.5394 | -0.0539 | -0.077 |
| □ | AgGaS2 | I42d | 2.5701 | 2.593 | -0.0229 | -0.0532 |
| ▲ | CsLiB6O10 | I42d | 1.5267 | 1.5943 | -0.0676 | -0.049 |
| □ | AgGaSe2 | I42d | 3.202 | 3.0058 | 0.1962 | -0.048 |
| □ | LiGaS2 | Pna21 | 2.296 | 2.2176 | 0.0784 | 0.042 |
|  | LiGaTe2 | I42d | 2.7982 | 2.7447 | 0.0535 |  |
| ▲ | LiB3O5 | Pna21 | 1.7313 | 1.6527 | 0.0786 | 0.041 |
| □ | BaMgF4 | Cmc21 | 1.5053 | 1.5538 | -0.0485 | 0.0278 |
| ▲ | SiO2 | P3121 | 2.6206 | 2.5394 | 0.0812 | 0.009 |
| ▲ | Al2O3 | R3c | 1.8305 | 1.8844 | -0.0539 | -0.008 |
| □ | Ba2TiSi2O8 | P4bm | 1.8138 | 1.8878 | -0.074 | -0.0003 |
|  | Li2B4O7 | I41cd | 1.7072 | 1.6042 | 0.103 | -0.0551 |
|  | ZrSiO4 | I41/amd | 2.1118 | 2.1201 | -0.0083 | 0.0305 |
|  | CaMgSi2O4 | C2/c | 1.7849 | 1.7951 | -0.0102 | 0.0275 |
|  | NaAlSi2O4 | C2/c | 1.7528 | 1.7502 | 0.0026 | 0.02 |
|  | LiAlSi2O4 | C2/c | 1.759 | 1.7559 | 0.0031 | 0.015 |
| ○ | Al2O(SiO4) | P1 | 1.8063 | 1.8262 | -0.0199 | -0.015 |
| ○ | BeAl2O4 | Pnma | 1.8485 | 1.8387 | 0.0098 | 0.009 |
|  | KAlSi3O8 | P1 | 1.6003 | 1.5958 | 0.0045 | -0.008 |
| □ | Al2Be3Si6O18 | P6/mcc | 1.6331 | 1.6438 | -0.0107 | -0.006 |

Among the above listed materials, birefringence was reproduced equally well by SOS and DFPT methods. We found DFPT improve significantly for those crystals that SOS give unsatisfactory results. We have proven that for some of such crystals, interestingly, SOS fails to reproduce the experimental birefringence simply because the electronic (optical) excitation does not break the symmetry, whereas DFPT does it correctly. There are two out of 28 crystals, symmetry-fixed DFPT agree with experiment even better than the full symmetry relaxed DFPT, but only slightly because the birefringence itself is small. We think that is accidental and not important.